## Slide 1
High-performance DIRC
Goal:
FY 19 progress:
A successful radiation hardness study was performed.
Purchase of two custom-made 3-layer lenses using sapphire and PbF2 as the middle layer is almost finalized.
The successful beam test of the PANDA Barrel DIRC prototype.
Very compact device with coverage up to 10 GeV/c for p/K, 6 GeV/c for /K, and 1.8 GeV/c for e/, pushing performance well beyond state-of-the-art
First DIRC aiming to utilize high-resolution 3D (x,y,t) reconstruction (performance and cost)

## Slide 2
3-layer lens
DIRC – overview
Radiation hardness test
Detailed radiation hardness study was performed at BNL, and five materials were tested up to 750 krad.
Sapphire and PbF2 were confirmed to be extremally radiation hard.
Radiation hard 3-layer lens prototypes
Both sapphire and PbF2 present new manufacturing challenges that have to be addressed by potential vendors.
Discussion are in final stage to finalize the purchase of two custom-made 3-layer lenses using sapphire and PbF2 as the middle layer.
Reducing sensors coverage
The successful beam test of the PANDA Barrel DIRC prototype identified the potential for a significant reduction in the number of sensors required to cover the detector plane.
Sapphire
PbF2

## Slide 3
60Co setup at BNL
Radiation damage quantified by measuring the transmission in the 190-800 nm range in a monochromator.
Five materials studied.
Sapphire and PbF2 great radiation hardness confirmed.
Radiation Hardness Test
Co60 Chamber
Tested samples
Monochromator

## Slide 4
60Co setup at BNL
Radiation damage quantified by measuring the transmission in the 190-800 nm range in a monochromator.
Five materials studied.
Sapphire and PbF2 great radiation hardness confirmed.
Radiation Hardness Test
Tested samples
Sapphire
PbF2

## Slide 5
60Co setup at BNL
Radiation damage quantified by measuring the transmission in the 190-800 nm range in a monochromator.
Five materials studied.
Sapphire and PbF2 great radiation hardness confirmed.
Radiation Hardness Test
Tested samples
S-YGH51 (NLaK33)
mRICH Fresnel lens

## Slide 6
The performance of new design ideas has been validated using the PANDA Barrel DIRC prototype at CERN PS
Larger sensor pixels, slower electronics than EIC DIRC: → prototype goal: 3σ /K separation @ 3.5GeV/c
Optics similar to EIC DIRC design: narrow bar, fused silica prism, 3-layer spherical lens.
Measured photon yield, Cherenkov angle resolution per photon (SPR), and per particle (Δθc), and /K separation power – all in good agreement with simulation (which is also used to predict the performance of the EIC DIRC)
CERN2018 data analysis in progress.
Sustained performance nevertheless a significant reduction in the number of sensors covering the detector plane was observed.
Impact of reducing number of sensors has to be tested in EIC simulation.
Reducing sensor coverage
MCP-PMT arrangement
Example of hit pattern
π/p separation power