## Slide 1: Frontiers of mid-IR lasers based on transition metal doped chalcogenides. Optically Pumped CO2 Lasers and Amplifiers
S. Mirov1,2, D. Martyshkin,1 V. Fedorov,1 K. Karki,1
I. Moskalev2, S. Vasilyev2, M. Mirov2, J. Peppers2, V. Smolski2
D. Tovey,3 J. J. Pigeon,3 S. Ya. Tochitsky,3 I. Ben-Zvi,4 and C. Joshi3,
I. Pogorelsky5, M. Polyanskiy5
1Department of Physics, University of Alabama at Birmingham, CH 310, 1300 University Blvd., Birmingham, AL 35294, USA
2IPG Photonics - Southeast Technology Center, 100 Lucerne Ln, Birmingham, Al 35211, USA
3University of California, Los Angeles
4Stony Brook University
5Brookhaven National lab
Author e-mail address: mirov@uab.edu
The work reported here partially involves intellectual property developed at the University of Alabama at Birmingham (UAB). This intellectual property has been licensed to the IPG Photonics Corporation. The UAB co-authors declare competing financial interests.
October 15, 2019 ATF Science Planning Workshop, LWIR Laser Capabilities
Funding:
Department of Energy (DOE) Office of Science Accelerator Stewardship award (DE-SC0018378)

## Slide 2: Outline
Motivation. Why Optically pumped CO2 lasers/amplifiers
TM:II-VI MIR laser materials introduction (Fe:Cr:ZnS/ZnSe )
Cr:ZnS/ZnSe oscillators and amplifiers
Fe:II-VI oscillators and amplifiers at 4-5 m
Fe:ZnSe pumped CO2 lasers/amplifiers
Conclusions and Outlook
001
100
000
4.3 mm
10 mm
CO2 Levels

## Slide 3: Ultrafast MIR laser sources : Motivation and Technologies
Goal: produce high power (1 TW), short (<1 ps) pulses in LWIR
Down conversion of near-IR lasers (Ti-S, Yb, Er) in (2), (3) materials
Well established near-IR fiber, bulk, thin disk fs lasers
Well established conversion techniques: OPCPA, DFG, OPO, SCG.
Complex setups, difficult to remain efficient for λ > 5 µm
Direct fs lasing in the MIR + OPCPA, DFG, OPO, SCG
Most compact, efficient, and high power fs sources
2 µm Tm-, Ho-doped bulk, thin disk, silica-based fiber lasers
3 µm Er-, Ho-doped fluoride-based fiber lasers
2—3 µm Cr:ZnS and Cr:ZnSe lasers
3.4—5 µm Fe:ZnS and Fe:ZnSe lasers
4—8 µm Fe:CdZnTe lasers
S. Mirov et al., IEEE JSTQE 24, 1601829 (2018)
A. Ongstad et al., SPIE Defense and Security, 2018
- A.D. Martinez et al., Opt. Mat. Express 5(9). 2036-2046 (2015).
I. Pupeza et al., Nature Photon. 9, 721 (2015).
J. Zhang et al., Light: Science & Applications 7, 17180 (2018)
M. Gebhardt et al., Opt. Lett. 42, 4179 (2017)
Room-temperature cross-sections of emission of
(i) Cr:ZnS, ii) Cr:ZnSe ; iii) Fe:ZnS, iv) Fe:ZnSe,
v) Fe:Cd0.75Mn0.25Se, vi) Fe:CdTe,
vii) Fe:Zn0.5Cd0.5Te, and viii) Fe:Cd0.5Mn0.5Te
55-80 μs radiative lifetime - High energy storage capability. Promising mid-IR amplifiers of ns-fs pulses!

## Slide 4: Alternative approach - optically pumped high pressure CO2 lasers/amplifiers
At 10 atm 2x35 GHz > 55GHz line spacing
col=3.5 GHz x atm
C
O
O
0001
0000
1000
10 mm
9 mm
0200
Boltzman Distribution
Normalized Ampl..
Wavelength (mm)
~1.2THz
~20 atm CO2
is desirable but
super difficult by
e- discharge
High pressure is needed for broad bandwidth amplification to broaden rotational spectral lines. Very difficult to operate electric discharge pumped CO2 lasers at high pressure.
Our solution: optically pumped CO2 lasers
4.3 μm pumping

## Slide 5: TM:II-VI materials: Introduction
TM dopants: Cr2+, Fe2+, Co2+, V2+, Mn2+, Ni2+
II-VI compounds: ZnSe, ZnS, CdSe, CdS, ZnTe, CdMnTe, CdZnTe, ZnSSe
Typical representatives: Cr and Fe doped ZnS and ZnSe
Features of II-VI semiconductors
Wide bandgap
Low phonon cutoff
Tetrahedral coordination
Features of Cr2+ and Fe2+ dopants
‘Right’ multiplet structure
Broad absorption and emission bands
High cross-sections
Absence of excited state absorption
TM:II-VI crystals being mid IR analogs of Ti:S are unique solution for Mid-IR Lasing
Energy Structure of Transition Metal Ions in ZnS
DeLoach et al., IEEE J. Quantum Electron., 32, 885 (1996).
S. Mirov et al., IEEE JSTQE 24, 1601829 (2018)

## Slide 6: Cr doped ZnSe and Cr:ZnS
Key Advantages
Access to 1.8 – 3.4 µm range
Convenient pumping by Er-, Tm- fiber lasers
Potentially electrically pumped
Room temperature operation
Other Features
Supports all laser regimes cw, ms, µs, ns, ps, fs
Direct pumping by laser diodes
Cr:ZnS (vs. Cr:ZnSe)
Very similar spectroscopically
Better thermo-optics
Broader bandgap (3.9 vs. 2.7 eV)
Lower nonlinearity (4 vs. 15 pm/V)
Key Advantages
Access to 3.4 – 5.2 µm range
Pumping by Cr:ZnS/ZnSe lasers
Other Features
Pumping at 2.94 µm by Er:YAG lasers
Pumping at 2.7 µm by HF lasers
Supports all laser regimes
cw, ms, µs at T < 220 K
ns at room temperature
mode-locked [work in progress]
60 s lifetime – high energy storage capability.
Q-switching and amplification of ns-fs pulses in the mid-IR
Fe:ZnS vs. Fe:ZnSe
Very similar spectroscopically
Fe doped ZnSe and ZnS

## Slide 7: Polycrystalline Cr2+:ZnSe, Cr2+:ZnS and Fe:ZnSe: Unique combination of parameters
Superb ultra-fast laser capabilities are blended with
High nonlinearity of II-VI semiconductors
Controllable polycrystalline microstructure that enables random quasi-phase matching (RQPM)
Fabrication technology that enables power scaling
Spinning ring – spinning cavity oscillator/amplifier platforms to control thermal management
I. Moskalev et al., Opt. Express 24, 21090 (2016)
S. Mirov et al., IEEE JSTQE 24, 1601829 (2018)

## Slide 8: Cr:ZnS/ZnSe lasers at 2-3 µm: State-of-the-art
Typical tuning curve of cw oscillator
CW regime
140 W (spinning ring technology, =62%)
ms, and µs pulses
1.1 J (at 0.1 Hz rep rate)
ns pulses
20 mJ (at kHz rep rate)
fs pulses
Highest average power 30 W
Highest peak power 8 MW
Highest pulse energy 400 nJ
Broadest range of repetition rates 75 MHz – 1.2 GHz
2 optical cycles (at multi-Watt power)
20 – 25% conversion efficiency
5 GW (1 mJ, 100 fs) Cr:ZnSe CPA

## Slide 9: SR Cr:ZnSe amplifier: Optimization for high average power
Output parameters of multi-cycle Spinning Ring Cr:ZnS + Cr:ZnSe MOPA
Seed pulses: 60 fs (8-cycle), 11 nJ at f = 81 MHz, P = 0.9 W
Output pulses: 60 fs, 0.34 µJ, P = 27.5 W, PPk = 5 MW
Cw TDFL → fs MIR conversion: 25% efficiency at G = 31
Measured output parameters of 28 W 60 fs SR MOPA

## Slide 10
Features of single-pass Cr:ZnSe energy amplifier
Seed pulses: 30 fs, 15 nJ, down-picking to 1 kHz
High single-pass gain (30 dB) + fs-SCG in bulk medium
Output pulses: 9 µJ with  = 41 (110) THz
Options for recompression to sub-2-cycle pulses with PPk = 1 GW
Measured spectra of seed (blue) and output (red) pulses
Schematic of single-pass energy amplifier
Single-pass energy amplifier (Cr:ZnSe) with high nonlinearity Goal: Sub-two-cycle MIR pulses

## Slide 12
Single-pass Cr:ZnS/Se amplifiers : Enabling Technology
 Spectrum of 3-octave VIS to MIR continuum 
 Detected fCEO signal
Simultaneous amplification, SCG, three-wave mixing via RQPM
Multi-octave frequency combs with Intrinsic nonlinear interferometry
Laser setup
S. Vasilyev et al, Optica 6(2), 126 (2019).

## Slide 13: Multi-Octave visible to long-wave IR femtosecond continuum generated in Cr:ZnS-GaSe tandem
Intrapulse DFG with Cr2+-based lasers
Perfect match for ZGP, GaSe, OP-GaP
Enables exceptionally efficient IDFG >5% in ZGP)
Enables exceptionally broadband and flexible IDFG (GaSe)
The obtained average power levels include several mW in the 0.4–0.8 µm visible, 0.23 W in the 0.8–2 µm near-IR, up to 4 W in the 2–3 µm IR, and about 17 mW in the 3–18 µm long-wave IR bands, respectively.
S. Vasilyev, et al., Optica 6(1), 111 (2019)
S. Vasilyev, et al., Optica (memorandum), 6(2), 126 (2019)
Cr:ZnS/Se fs oscillators and amplifiers are enabling technology for frequency combs covering 2-20 m spectral range!!!
Advantages over near IR pump for IDFG:
IDFG efficiency ~Leff2 ;
Limiting factor - group velocity mismatch between pump and mid-IR pulses. It narrows down when the pump wavelength increases.
For GaSe , assuming IDFG center wavelength ~ 10 µm and pump pulse duration 15 fs, Leff = 22 µm for 1-µm pump and as large as 1.5 mm for 2.5 µm pump. With the Leff2 scaling, shifting to a longer wavelength pump gives 5,000 times increase in the IDFG conversion efficiency.
Access to NL materials with broad mid-IR transparency and high figure of merit.

## Slide 14: Fe:ZnS/ZnSe lasers at 3-5 µm : State-of-the-art
CW regime
10 W (77 K)
ms, and µs pulses
10.5J (77 K)
ns pulses
1.6 J single pulse (RT) K. Firsov et al.,
Applied Physics B (2016)
fs pulses Work in progress
S. B. Mirov et al., IEEE J. of Sel. Topics in Quantum Electron. 24, 1601829 (2018) DOI: 10.1109/JSTQE.2018.2808284.
Output-Input of cw Fe:ZnSe laser
High power (35 W, 100 Hz) pulsed Fe:ZnSe laser Pulsed, RT (1 mJ @5 ns@1 kHz) Fe:ZnS laser CW, 10W, 3.7-5 um tunable Fe:ZnSe
Tuning curve of pulsed RT Fe:ZnSe laser

## Slide 15
UCLA
20 atm Optically Pumped CO2 Laser
We will combine the best of gas laser and SSL technologies to generate a~1ps, 100 GW LWIR pulses: dramatic reduction of size and amplification of shorter pulses. Ultimate goal is a compact TW power CO2 laser pumped by 4.3 mm Fe:ZnSe laser.
001
100
000
4.3 mm
10 mm
CO2 Levels
Collaboration between UCLA/BNL/UAB
20 atm
12CO2--13CO2—He
Gain Spectrum
4.3 mm
Fe:ZnSe
Laser
10 mm
1 ps, 10-100 GW
10 mm
500 fs
OPA
Seed

## Slide 16: Picosecond CO2 Regenerative Amplifier (simulations)
10 mm Seed:10 μJ
300 fs - 500 fs
UCLA
10cm-long picosecond amplifier
4.3 mm Pump: 200-300 mJ, pulse from Fe:ZnSe laser
20 atm
CO2 cell
Feasibility study of a compact GW class CO2 amplifier at 20 Hz.
D. Tovey et al. Applied Optics, 58, 5756-5763, 2019
IN
OUT

## Slide 17: Fe:ZnSe 4.3 µm Pump Laser
Tunable across entire 4.3 µm absorption branch of CO2
Produces ~2-3 mJ, ~40 ns pulses at 10 Hz rep rate
Laser Setup
Tuning Curve
V. Fedorov, et. al., Opt. Express 27(10), 13934-13941 (2019)

## Slide 18
Optically Pumped CO2 Laser 0.2 atm
UCLA
MARS
Pump 2 mJ Fe:ZnSe laser, Optical-to-optical 10 mm/4.3 mm≤30%.
Need 200-300 mJ for 20 atm CO2 laser. D. Tovey et al, CLEO, 2019, paper STh1E4

## Slide 19
UCLA
1 J
1 ps
MARS
10 Hz 4.3 mm
Fe:ZnSe Laser
10 Hz 4.3 mm
Fe:ZnSe amplifier
~mJ
0.5 ps
Mode-locked
20 atm OPCO2
Laser
20 atm
OPCO2
Preamp
20 atm
OPCO2
Amplifier
10 mJ
1 J
3 J
4 J
100 ns
+++) Table-top electrical discharge-free compact TW LWIR
laser system will be suitable for self-guiding in air over km range, etc.
+++) Optical-to-optical conversion efficiency 0.1-0.4 is far above
any state-of-the-art LWIR OPA.
- - - ) Physics of Optically Pumped high-pressure CO2 medium needs to be studied.
Optically pumped high-pressure CO2 lasers can be the game changer in LWIR USP:100 ns pump and 0.3-3 ps LWIR pulse.
At present our goal is GW level of power from OP CO2 laser and only after reaching this goal one can consider a higher TW powers. More energetic Fe:ZnSe systems and Fe:ZnSe pump sources are needed.
Even higher power of 10-20 TW we leave to existing discharge pumping.
Compact OP CO2 TW Laser

## Slide 20
Home-made Er:YAG 25 J at 2940 nm
pumping
Fe:ZnSe output energy 7.5J at 220K
(10.6J at 77K)
Fe:ZnSe rep rate – single pulse
Pulse duration 700 s
Efficiency 30%

## Slide 21
nonchain electric-discharge
HF laser pumping
Fe:ZnSe output energy 1 J
Fe:ZnSe rep rate 20 Hz
Fe:ZnSe output power 20W
Pulse duration 150 ns
RT operation with efficiency 40%

## Slide 22
Multipass RT Fe:ZnSe amplifier feasibility

## Slide 23
Er:YAG@2.9 µ /2J/100µs/10Hz
SM
Nitrogen
Cryostat
SM
SM
0.3J@2.9µm
SM
0.5.J @2.9µm
1.2J@2.9µm
SM
1 mJ@4.1µm
Low temperature Fe:ZnSe long-pulse (100 s) pumped amplifier
 3x0.5cm Fe:ZnSe gain element developed at the UAB
1 stage Fe:ZnSe 2x1019 cm-3
1 stage amplifier Fe:ZnSe 2x1019 cm-3 pumped by 0.3J at 2.9 um
2nd stage amplifier Fe:ZnSe 6x1018 cm-3 pumped by 0.5J at 2.9 um
2nd stage Fe:ZnSe 6x1018 cm-3
10mJ@4.1µm
500mJ@4.1µm
150mJ@4.1µm

## Slide 24: Principal laser scheme based on Electro-Optical QS Nd:YAG@ 1.064 m
2.94 m
1.064 m
OPO KTA
EO QS Nd:YAG laser
F:ZnSe
Tunable Laser
F:ZnSe
Amplifier
Free Running Er:YAG
48’’
LN
Tank
24’’
3.0 m
3.9-5.0 m
3.9-5.0 m

## Slide 25: Mechanically Q-switched (spinning mirror) Er:YAG laser @ 2.94 µm
10 mm Er:YAG 50%
BM
OC 75%
Flash Lamp Driver
Pulse Generator
f~ 600Hz
f/60
He-Ne laser
PD
2.94 m
365 mm
Power Meter
DC, Motor | 
Nominal Voltage | 24 V
Nominal torque | 20mNm
Nominal speed | 55600 rpm

## Slide 26
Dimension of rod: 7mm * 120 mm
Cavity length = 365mm. PRR = 5Hz
Laser driver: KALD Megawatt laser
Temperature of chiller = 170 C
Mechanically Q-switched (spinning mirror) Er:YAG laser
Chart: Pump (J)
| 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50
Output(FR) | 0 | 4 | 12 | 25 | 42 | 66 | 97 | 130 | 172 | 220 | 300 | 380 | 460 | 550 | 640
Output (QS) | 0 | 11 | 36 | 56 | 106 | 154 | 196 | 220 | 260
Maximum output energy in a single pulse = 260 mJ (mirror damage limited)

## Slide 27
Optically pumped high pressure CO2 offers potential for compact, efficient generation/amplification of high power, picosecond pulses at 10 µm
Experimental demonstrations of low pressure lasing in CO2 pumped by an Fe2+:ZnSe laser indicate high optical- optical conversion efficiencies are possible
Scaling to higher pressure requires better understanding of physics behind CO2 lasing (self-focusing of pump, CO2 relaxation processes) and/or more energetic pump source
Plan to submit DOE proposal to demonstrate and optimize a short pulse OP lasers, focusing on a shorter pulse length down to 300 fs, and power scaling.
Summary and outlook

## Slide 28
Laser regime | Cr:ZnSe/ZnS,  = 1.8 – 3.4 µm | Fe:ZnSe/ZnS,  = 3.4 – 5.2 µm
Continuous wave | 140 W with 60% efficiency (RT) | ~ 10 W (77 K)
ms pulses | 1.1 J (single-shot) (RT) | 10.6J
µs pulses | NA | 0.35 J at 100 Hz (77 K)
ns pulses | 20 mJ at 1000 Hz (RT) | 1.6 J at single pulses (RT)
fs pulses | <20 fs, up to 30W (RT) | < 1 ps (77K)
THANK YOU FOR YOUR ATTENTION

## Slide 29: Cr2+:ZnSe and Cr2+:ZnS: laser and nonlinear materials
(2)
High d36  20 pm/V
All types of three-wave mixing via RQPM
SHG, SFG, OPO, DFG/IDFG
(3)
High n2  10-14 cm2/W at  = 2.4 µm
Low critical power for self-focusing PCrit = 0.4 MW at 2.4 µm
2—3 µm lasing in normal group velocity dispersion (GVD) regime
GVD  0 fs2/mm at 3.6 µm (ZnS) and at 4.81 µm (ZnSe)
(3) + (2) + RQPM = multi-octave SCG
Different regimes of three-wave mixing
Harmonics-enhanced SCG in ZnSe pumped by a µJ kHz CPA R. Šuminas et al., JOSA B 36, A22 (2019)
R. Šuminas et al., Appl. Phys. Lett. 110, 241106 (2017)

## Slide 30: TM:II-VI materials: Fabrication
S.B. Mirov, V.V. Fedorov, (November 1, 2005) Mid-IR microchip laser: ZnS:Cr2+ laser and saturation absorption material”, US Patent No 6,960,486
Single crystals by Bridgman technique
Requires high temperature, pressure (e.g. 1600 K at 75 bar)
Single crystals by chemical vapor transport (CVT) and physical vapor transport (PVT) methods
Hard to reach high dopant concentration
Hard to get good optical quality
Hard to grow large size crystals
Polycrystalline by post-growth thermal diffusion doping
Uniformly-doped, large samples with high dopant concentration
Mass-production of the gain elements with pre-assigned parameters
Hot-pressed ceramics
Enables engineering of the parameters (dopant distribution, microstructure)
Promising future technology
Nano & micropowders, composite II-VI-liquid, II-VI-polymer and II-VI-glass gain media

## Slide 31: Approaches to super-octave sub-2-cycle Cr2+:ZnS and Cr2+:ZnSe lasing
Standard technique →
N. Tolstik et al., Proc. SPIE 8599 (2013) Chalcogenide and germanate fiber
S. Xie et al., Opt. Express 24, 12406 (2016) As2S3-silica double-nanospike waveguide
D. Martyshkin et al., Opt. Mater. Exp. (2019) Silicon nitride waveguide
N. Nagl et al., Opt. Lett. (2019) fluoride fibers
Singe-pass Cr:ZnS and Cr:ZnSe amplifiers “All-in-one” bulk architecture
S. Vasilyev et al., Opt. Express 22 , 5118 (2014)
S. Vasilyev et al., Opt. Express 24, 1616 (2016)
S. Vasilyev et al., Opt. Mat. Express 7, 2636 (2017)
→
Concept of a single-pass TM:II-VI amplifier

## Slide 32: Single-pass ultrafast Cr:ZnS and Cr:ZnSe amplifiers
Main features
Simple yet efficient
ab = 1.110-18 cm2
 = 5.4 µs
ISat = 20 kW/cm2
FSat = 0.1 J/cm2
Variety of options for optical pumping
EDFLs (cw)
TDFLs (cw)
Er:YAG, Ho:YAG, Ho:YLF (ns)
Great flexibility:
f = repetition rate = 100 – 109
 = Pump/Seed = 100 – 106
 = Ppk/PCrit = 10-2 – 102
Generic single-pass power amplifier at full repetition rate
Generic single-pass energy amplifier at kHz—MHz repetition rate

## Slide 33: Single-pass fs amplifier (Cr:ZnS) at GHz repetition rate Goal: Compactness-&-Efficiency
Features of GHz fs Cr:ZnS MOPA
Seed pulses: 80 fs, 1 nJ at f = 0.9 GHz, P = 0.9 W
Output pulses: 76 fs, 8 nJ, P = 7.3 W (100 kW peak power)
Cw EDFL → fs MIR conversion: 38% amplifier (31% overall)
Footprint: 20×20 cm2 (excluding EDFLs)
Ideal pump for subharmonic fs OPOs:
→
Parameters of 7.3 W MIR fs source at 0.9 GHz repetition rate
V. Smolski et al., ASSL2017, AM4A.6
GHz power amplifier

## Slide 34
Middle-IR lasers based on Cr and Fe doped ZnS and ZnSe have come of age
Advances in fabrication of ceramic/polycrystalline laser materials
Availability of cost efficient fiber pump lasers at 1.5—2 µm
Advances in laser design and thermal management
Important milestones have been reached
0.15 kW level in cw laser power
>J-level energy
Summary and outlook
Ultrafast Cr2+-based lasers and amplifiers provide unique combination of parameters in the spectral range 2—3 µm
Short Pulses: 2—3 optical cycles (Outlook sub-2 cycle)
High power: in excess of 27 W (Outlook 100 W)
Very high efficiency : 20 – 40 % conversion from cw EDFL and TDFL to fs MIR

## Slide 35
Summary and outlook
Cr2+:ZnS(Se)—GaSe tandems enable generation of 5-octave (0.4—20 µm) continua
First bulk, multi-octave continuum at full 80 MHz repetition rate of a fs oscillator
First implementations of new SCG regimes:
Harmonics-enhanced supercontinuum generation in RQMP media
IDFG-enhanced supercontinuum generation
Direct fCEO measurements confirm high spatio-temporal coherence of the continuum
Future TW-class Cr,Fe:ZnS/ZnSe and Fe:ZnS/ZnSe/ZnCdTe amplifiers at 2 – 8 µm
Future electrically pumped TM:II-VI lasers
Increasing interest from various fields
Spectroscopy and sensing
Processing of materials
Medicine-, defense-related applications, etc.
Strong field physics and nonlinear optics, atto-science