## Slide 1: LQXF Coil Winding and Curing Cable Re-spooling at FNAL
Miao Yu
05/06/2014

## Slide 2: Cable Re-spooling Setup
Digital counter, measures in meters and tenths
Tension is provided by payout and respooler

## Slide 3: Tension Control
Tension can be adjusted by tuning the input voltage to both respooler and payout

## Slide 4: Re-spooling
Cable total length verification
Insulation and cable inspection visually
Mark the split position for L1 and L2 cable (minimum length, L1 = 184 m; L2 = 233 m)
Take the full spool off the respooler, and put an empty reel on the respooler. Split into two spools.
Use die cart to transfer two spools together.

## Slide 5: LQXF Coil Winding and Curing Winding with Rotation Table at FNAL
Miao Yu
05/06/2014

## Slide 6: Rotation Table
4.3 m long support frame, need modification. Current frame to tension distance: 1.5 m
Winding table was used for 3.4 m LHQ coil. Need load verification for 4.5 m long LQXF coil at 55 lbs winding tension.
All the work will start this summer.

## Slide 7: Frame Modification
4.85 m long frame for 4.5 m LQXF coil
Work including cutting, alignment, welding

## Slide 8: Winding Mandrel
For SQXF Coil
Extended for LQXF

## Slide 9: Winding Tooling
For SQXF Coil
Adopted for LQXF

## Slide 10: Curing Tooling
SQXF Coil
Duplicate for LQXF
Selva support beam
Winding mandrel support can be bolted to the beam

## Slide 11: LQXF Coil Winding and Curing Curing Process at FNAL
Miao Yu
05/06/2014

## Slide 12: Curing Mold
2.2 m SQXF curing mold is in service
8.8 m LQXF curing mold will be built in the end of this year.

## Slide 13: Curing Press
 | Capacity (pump psi) | Max. force/cylinder kN (ton) | Spacing cm(inch) | Unit force kN/m-pump psi (lb/in-pump psi)
Main Cylinders | 10000 | 1780 (200) | 30 (12) | 0.6 (3.34)
Mandrel Cylinders | 10000 | 134 (15) | 15 (6) | 0.09 (0.5)
8.8 m long

## Slide 14: Curing Pressure Control
For SQXF Coil, the azimuthal stress is well controlled ~10 MPa
L1
L2

## Slide 15: Pressure Control Panel

## Slide 16: Temperature Control
Once the curing mold is closed, start heating the mold
Keep the hydraulic pressure during the thermal cycle.

## Slide 17: Coil Axial Load and Alignment
Both ends are pushed by the rods with or without the rubber before curing.
During curing, no additional action.
L1: one pin through the tooling, to the coil
L2: two screws to the lifting holes in the coil

## Slide 18: LQXF Coil Winding and Curing Coil Handling
Miao Yu
05/06/2014

## Slide 19: During W&C
For SQXF Coil
For LQXF Coil

## Slide 20: After Curing
For SQXF
LQXF