## Slide 1: SQXF Coil QA and Measurement during Winding and Curing
Miao Yu
05/05/2014

## Slide 2: QA and Measurement for Coil1
Monitoring coil to ground short
Coil to parts electrical short test
Coil electrical measurement after winding and curing (R, Ls, Q)
Winding mandrel rotation angle
Each turn cable measurement during winding (angle and location at the end nose)
Coil measurement after winding and after curing (coil length, coil end)
Pole gap and wedge gap

## Slide 3: Coil to Ground/Part Short Test
Ω meter is set up to monitor cable to ground short through the winding
Connect each end part to ground to check part to cable short
  After installing wedges
  After finishing winding
  After finish curing

## Slide 4: Coil Electrical Measurement
Resistance: from IL lead to OL lead
  SQXF coil 1: 0.164 Ω
Inductance and Q value
 | 20 Hz | 120 Hz | 1 kHz
Ls (mH) | 3.298 | 3.085 | 2.305
Q | 2.26 | 5.32 | 3.02
SQXF Coil 1

## Slide 5: Winding Mandrel Rotation
The mandrel angle is measured at exit position when the cable wind around the end
This angle remain constant when the cable wind along the straight section

## Slide 6: Each turn cable measurement

## Slide 7: Coil measurement
IL
OL
Coil end measurement
  Install pins
  Measured with caliper between the edges of pins
  Subtract by the radii of the pins
  Record the distance
Coil length
  Measure the overall length of the winding mandrel
  Measure the distance between RE saddle and RE of the winding mandrel
  Measure the distance between LE splice block and LE of the winding mandrel
  Subtract 1 by 2 and 3
  Record the coil length

## Slide 8: Pole Gap and Wedge Gap
Measured with caliper
Pole gap
  Original gap (L1)
  After winding (L1 and L2)
  After curing (L1 and L2)
  After release tension (L2)
  After reaction (L2)
Wedge gap
  Original gap = minimum pole gap + 3 mm
  After winding
  After curing
  After release tension
  After reaction