## Slide 1: FY20 Thermal Neutron Scattering Measurements at the ORNL Spallation Neutron Source
Chris W. Chapman1, Xunxiang Hu1, Jesse Brown1, Goran Arbanas1, Kemal Ramić2, Alexander I. Kolesnikov1, Yongqiang Cheng1, Luke Daemen1, Anibal Ramirez Cuesta1, Doug Abernathy1, Li (Emily) Liu2, Yaron Danon2
1Oak Ridge National Laboratory 2Rensselaer Polytechnic Institute
CSEWG – US National Nuclear Data Week 2020 30 November – 2 December 2020 - Online

## Slide 2: Overview
Spallation Neutron Source (SNS)
  Facility layout
  Instruments used
Measured materials
  Yttrium hydride
  Polystyrene
Conclusions

## Slide 3: SNS Overview
High-energy protons accelerated to 1 GeV
  1.4 MW LINAC
Neutron produced by spallation with mercury target
  Pulsed neutrons produced at 60 Hz
Neutrons thermalized by passing through water moderator
Peak brightness: ~1 × 1013 n/cm2/sr/Å/s

## Slide 4: SNS Overview

## Slide 5: SNS Overview

## Slide 6: SNS: ARCS & SEQUOIA
Time-of-flight direct geometry spectrometer
User chooses incident energy; Fermi choppers rotate to collimate white beam to selected energy
Detector setup measures final energy and scattering angle
  SEQUOIA: slightly better energy resolution
  ARCS: larger angular range

## Slide 7: SNS: VISION
Indirect geometry vibrational spectrometer
White beam of neutrons hits target
Scattered neutrons reflected off graphite blocks to two detectors for forward- and backward-scattering angles
Graphite blocks configured to scatter neutrons at 4 meV
Constant relative energy resolution

## Slide 8: SNS: (Q,E) Grid of Direct and Indirect Spectrometers
Direct Geometry Spectrometer (ARCS)
Indirect Geometry Spectrometer (VISION)

## Slide 9: YHx Overview
Moderator of choice for Oak Ridge National Laboratory (ORNL) Transformational Challenge Reactor (TCR)
Measurement is two-fold:
  Hydrogen concentration
  Anharmonicities at high temperatures
Modeling efforts in corresponding talk
  “Modeling of Anharmonic Effects and Temperature Depencency of the YH2 Phonon Spectrum,” by Kemal Ramić

## Slide 10: YHx Overview
SNS instrument | Samples | Sample form | Sample fixture | Mass (g) | Incident neutron energy (meV) | Temperature (K)
SEQUOIA | YH1.62 | Powder | Aluminum plate and cover | 0.6966 | 45, 180, 600 | 5
 | YH1.86 |  |  | 0.702 |  | 5, 295, 550, 800
VISION | YH1.62 |  |  | 0.6966 | N/A | 5, 293
 | YH1.74 |  |  | 0.6684 |  | 
 | YH1.86 |  |  | 0.702 |  | 
 | YH1.90 |  |  | 0.7696 |  | 
ARCS | YH1.68 | 0.1 mm hydride foil | Thin-wall quartz tube | 1.6681 | 45, 180, 600 | 295, 550, 800, 900, 1,000, 1,100, 1,200
 | YH1.87 |  |  | 1.8937 |  | 

## Slide 11: YHx: ARCS/SEQUOIA Comparison

## Slide 12: YHx: SEQUOIA measurements

## Slide 13: YHx: ARCS Measurements—Temperature Comparison

## Slide 14: YHx: VISION Measurements

## Slide 15: YHx: VISION Measurements

## Slide 16: Polystyrene Overview
Nuclear Criticality Safety Program material of interest; used in several International Criticality Safety Benchmark Evaluation Project benchmarks
Previously used polyethylene as a surrogate
Scientific merit:
  Molecular weight
  Tacticity
  Crystal vs. amorphous

## Slide 17: Polystyrene Overview
Material | MW | Incident neutron energy (meV) | Temperature (K)
Syndiotactic Polystyrene (sPS) | 6,400 | 40, 100, 225, 500 | 5, 293
 | 31,600 | 40, 100, 225 | 5
 | 171,000 |  | 
 | 965,000 | 40, 100, 225, 500 | 5, 293
Atactic Polystyrene (aPS) | 5,800 | 40, 100, 225, 500 | 5
 | 25,000 |  | 
 | 170,000 |  | 
 | 650,000 |  | 

## Slide 18: Polystyrene: Comparison with Polyethylene

## Slide 19: Polystyrene: sPS Molecular Weight Comparison

## Slide 20: Polystyrene: Tacticity Comparison

## Slide 21: Conclusions
YHx
  Anharmonicities play significant role in inelastic spectra
Polystyrene
  Inelastic spectra different from polyethylene
  No noticeable difference in inelastic scattering as a function of MW or tacticity for amorphous samples
  Further measurements planned to determine effect of crystallinity

## Slide 22: Acknowledgments
This research was sponsored by the TCR program of the US Department of Energy’s (DOE’s) Office of Nuclear Energy.
This work was supported by the Nuclear Criticality Safety Program, funded and managed by the National Nuclear Security Administration for the Department of Energy
This research used resources at the SNS, a DOE Office of Science User Facility operated by ORNL.

## Slide 23: Questions?