## Slide 1
Strand design, status and plans by CERN
B. Bordini, A. Ballarino, L. Oberli
Brookhaven National Laboratory, – 8th May 2014
LARP CM22/ HiLumi-LHC Collaboration Meeting

## Slide 2: Outline
Nb3Sn procurement: status and plans
CERN experience with the RRP 132/169
  The 1 mm wire for the FRESCA2 magnet
  The 0.85 mm wire for the QXF magnets
  Cabling the QXF conductor
  Magnetization of the 0.85 mm wire
Scaling the Nb3Sn critical current at 1.9 K

## Slide 3: Nb3Sn Procurement
100 km PIT Dipole
20 km +20 km Quadrupole
1.087 t Fresca2
1.364 t Dipole
0.578 t Quadrupole
Quadrupole
Long Prototype
Dipole
Series
Dipole
Series
Quadrupole
Series
Orders of conductor for prototype dipole magnets completed

## Slide 4: QXF Nb3Sn Procurement
Procured
Partially Procured
Short Model Program
Planned
Long Prototypes
2012
2013
2014
2015
2016
Cabling trials: 5+5 km
SMP: 35+35 km
SMP: 20+20 km
LP: 200+200 km
2017
Conductor
for series
Practice coils
SMP: 7+7 km
Practice coils
LMP: 30+30 km
6+6 SMCs
6+6 LMCs
5+5 SMCs (May 2015)
Ordered
The procurement is proceeding as planned – conductor review October 2013

## Slide 5: Conductor for CERN projects
 | Sub-element size (m) |  |  |  |  | 
 | Wire  (mm) | RRP 108/127 | RRP 132/169 | RRP 192/217 | PIT 114 | PIT 192
FRESCA 2* | 1 | - | 58 | - | - | 48
Hi-Lumi Quad | 0.85 | - | 48 | - | - | 41
11 T | 0.7 | 46 | 41 | 32 | 44 | -
*Fresca 2 conductor: procurement by CERN and CEA – FP7 European Project
RRP
54/61
108/127
132/169
198/217
PIT
114
192

## Slide 6: Km of Wire Received at CERN
 | Quantity Procured (km) |  |  | 
 | Wire  (mm) | RRP 132/169 | PIT 114 | PIT 192
FRESCA 2 | 1 | 10+15+18+45 | - | 1+9+15+15+45
Hi-Lumi Quad | 0.85 | 5 + 35 | - | 5 + 5 + 37
11 T | 0.7 | 30 +28+ 122 | 3 + 22.4*+43+ 7 | -
Delivered
In production at OST - (total quantity by Aug. 2014)
In production at Bruker - (delivery completed in June 2014)
In production at Bruker - (delivery completed in September 2014)
* Additional length of 12.2 km of PIT 192, 0.778 mm diameter, procured by CERN for LARP – shipped by CERN to LBNL in June 2013

## Slide 7: 1 mm 132/169 RRP Wire: Jc @ 15 T, 4.22 K
Chart: Billet Number
| 15949.0 | 15952.0 | 15955.0 | 15956.0 | 15958.0 | 15954.0 | 15957.0 | 15959.0 | 15961.0 | 15964.0
 | 1522 | 1543 | 1521 | 1533 | 1482 | 1534 | 1517 | 1470 | 1481 | 1458 | 1536 | 1481 | 1514 | 1454 | 1497 | 1481 | 1497 | 1491 | 1519 | 1577 | 1486 | 1538 | 1588 | 1543 | 1470 | 1515 | 1539 | 1477 | 1409
HT: 50 hours at 650 C
Chart: Billet Number
| 14310.0 | 14311.0 | 14312.0 | 14108.0 | 14393.0 | 14839.0 | 14840.0 | 14842.0
 | 1569 | 1627 | 1627 | 1698 | 1624 | 1627 | 1562 | 1557 | 1595 | 1612 | 1599 | 1644 | 1609 | 1641 | 1655 | 1540 | 1579 | 1599 | 1646 | 1641 | 1604 | 1617 | 1644 | 1594
Average, (A/mm2) | 1612.9
RMS, (A/mm2) | 35.9
RMS/Ave, % | 2.2
Min, (A/mm2) | 1540.0
Average, (A/mm2) | 1506.0
RMS, (A/mm2) | 38.3
RMS/Ave, % | 2.5
Min, (A/mm2) | 1409.0
Different Nb raw material

## Slide 8: 1 mm 132/169 RRP Wire: Jc @ 12 T, 4.22 K
Chart: Billet Number
| 14310.0 | 14311.0 | 14312.0 | 14108.0 | 14393.0 | 14839.0 | 14840.0 | 14842.0
 | 3020 | 3047 | 3026 | 3119 | 3098 | 3071 | 2967 | 2983 | 3040 | 3102 | 3028 | 3090 | 3006 | 3057 | 3102 | 2947 | 2943 | 3016 | 3040 | 3051 | 3013 | 3025 | 3058 | 3026
Chart: Billet Number
| 15949.0 | 15952.0 | 15955.0 | 15956.0 | 15958.0 | 15954.0 | 15957.0 | 15959.0 | 15961.0 | 15964.0
 | 2874 | 2907 | 2877 | 2887 | 2849 | 2883 | 2864 | 2793 | 2827 | 2777 | 2864 | 2822 | 2867 | 2801 | 2850 | 2811 | 2833 | 2786 | 2887 | 2948 | 2859 | 2928 | 2954 | 2920 | 2831 | 2874 | 2904 | 2862 | 2767
Average, (A/mm2) | 3036.5
RMS, (A/mm2) | 47.3
RMS/Ave, % | 1.6
Min, (A/mm2) | 2943.0
Average, (A/mm2) | 2858.8
RMS, (A/mm2) | 49.1
RMS/Ave, % | 1.7
Min, (A/mm2) | 2767.0
HT: 50 hours at 650 C
Different Nb raw material

## Slide 9: 1 mm 132/169 RRP Wire: Copper Residual Resistivity Ratio (RRR)
Chart: Billet Number
| 15949.0 | 15952.0 | 15955.0 | 15956.0 | 15958.0 | 15954.0 | 15957.0 | 15959.0 | 15961.0 | 15964.0
 | 248 | 268 | 242 | 224 | 230 | 277 | 276 | 280 | 295 | 260 | 302 | 281 | 255 | 263 | 301 | 285 | 311 | 322 | 300 | 300 | 311 | 302 | 327 | 338 | 318 | 327 | 290 | 280 | 299
Chart: Billet Number
| 14310.0 | 14311.0 | 14312.0 | 14108.0 | 14393.0 | 14839.0 | 14840.0 | 14842.0
 | 248 | 243 | 256 | 269 | 278 | 258 | 273 | 245 | 268 | 224 | 202 | 254 | 229 | 193 | 213 | 201 | 241 | 218 | 222 | 250 | 288 | 222 | 263 | 230
HT: 50 hours at 650 C
Average, (-) | 241.2
RMS, (-) | 25.9
RMS/Ave, % | 10.7
Min, (-) | 193.0
Average, (-) | 286.6
RMS, (-) | 29.4
RMS/Ave, % | 10.2
Min, (-) | 224.0
Different Nb raw material

## Slide 10: 1 mm 132/169 RRP Wire: Piece Lengths
59 % in lengths > 2000 m
Chart: No. of Pieces
14108 | 3312 | 891 | 781 | 577
14163 | 4246 | 670 | 207 | 188
14310 | 1200 | 654 | 577 | 472
14842 | 1568 | 1199 | 924
14311 | 1154 | 846 | 712 | 581 | 502
14312 | 2475 | 1179 | 533
14393 | 768 | 493
14839 | 2360 | 1219
14840 | 2560 | 1830 | 415
15949 | 4173 | 1063
15952 | 2154 | 1135
15955 | 3040

## Slide 11: 0.85 mm 132/169 RRP Wire: Ic @ 15 T, 4.22 K
Chart: Billet Number
| 14310.0 | 14393.0 | 14839.0 | 14842.0 | 15948.0 | 15960.0 | 15962.0 | 16277.0
 | 364 | 387 | 357 | 362 | 370 | 363 | 391 | 385 | 381 | 358 | 396 | 353 | 357 | 370 | 369 | 362 | 370 | 360 | 365 | 370
Chart: Billet Number
| 15914.0 | 15915.0
 | 368 | 365 | 355 | 366 | 377 | 360
Spec., (A) | 361
Average, (A) | 365.2
RMS, (A) | 7.5
RMS/Ave, % | 2.0
Min, (A) | 355.0
Min-Spec, % | -1.7
Low Tin
HT: 50 hours at 640 C
Spec., (A) | 361
Average, (A) | 368.5
RMS, (A) | 11.4
RMS/Ave, % | 3.1
Min, (A) | 353.0
Min-Spec, % | -2.2

## Slide 12: 0.85 mm 132/169 RRP Wire: Ic @ 12 T, 4.22 K
Chart: Billet Number
| 15914.0 | 15915.0
 | 708 | 707 | 694 | 712 | 723 | 699
Chart: Billet Number
| 14310.0 | 14393.0 | 14839.0 | 14842.0 | 15948.0 | 15960.0 | 15962.0 | 16277.0
 | 715 | 732 | 714 | 718 | 719 | 722 | 747 | 745 | 731 | 711 | 745 | 693 | 709 | 718 | 716 | 714 | 719 | 700 | 705 | 709
Average, (A) | 719.1
RMS, (A) | 14.6
RMS/Ave, % | 2.0
Min, (A) | 693.0
Average, (A) | 707.2
RMS, (A) | 10.1
RMS/Ave, % | 1.4
Min, (A) | 694.0
Low Tin
HT: 50 hours at 640 C

## Slide 13: 0.85 mm 132/169 RRP Wire: Copper Residual Resistivity Ratio (RRR)
Chart: Billet Number
| 14310.0 | 14393.0 | 14839.0 | 14842.0 | 15948.0 | 15960.0 | 15962.0 | 16277.0
 | 201 | 203 | 220 | 202 | 217 | 181 | 224 | 217 | 197 | 213 | 199 | 172 | 208 | 202 | 174 | 198 | 204 | 215 | 212 | 223
Chart: Billet Number
| 15914.0 | 15915.0
 | 330 | 325 | 313 | 286 | 285 | 317
Average, (-) | 204.1
RMS, (-) | 14.9
RMS/Ave, % | 7.3
Min, (-) | 172.0
Average, (-) | 309.3
RMS, (-) | 19.4
RMS/Ave, % | 6.3
Min, (-) | 285.0
Low Tin
HT: 50 hours at 640 C

## Slide 14: Cabling the QXF conductor based on the 132/169 RRP wire
Several Cables with different parameters were fabricated at CERN
In order to assess the critical current degradation due to cabling, extracted wires were systematically measured
Generally the degradation was limited to less than 5 % despite the strand looked significantly deformed on the thin edge
The wire is extremely robust in term of Ic degradation, at the moment the cabling program is focusing on to:
  Maintain the local RRR above 100
  Manufacture a mechanical stable cable

## Slide 15: Magnetization at 1.9 K of QXF wires: the 132/169 RRP vs the 192 PIT
Chart: Applied Field, [T]
Jc(12 T, 4.2 K) =2800 A/mm2
RRR=189
Jc(12 T, 4.2 K) =2500 A/mm2
RRR=136
With respect to the PIT wire, the RRP wire has:
  A significantly larger magnetization
  Bigger Flux Jumps
  A wider unstable region (2.5 T instead of 1.5 T)
Measurements by D. Richter – CERN TE/MSC/SCD

## Slide 16: The 132/169 RRP wire - Summary
When passing from a 0.7 mm wire to a 0.85 mm wire, the 132/169 is the natural evolution of the 108/127 (the historical layout used by the LARP collaboration) in order to maintain similar sub-element size
  Limit the magnetization and the low field instabilities
  Similar sub-element design and heat treatments
CERN has a significant experience with the 132/169 wire: 88 Km of wire were procured for the FRESCA2 magnet and 40 km for the QXF magnets
All the wire received at CERN satisfies the current specification with significant margin for the RRR specification

## Slide 17: Critical Current QXF RRP Wire
Chart: Peak Field, (T)
| 16.14 | 15.18 | 14.22 | 13.27562376470588 | 12.33730529411765 | 11.4078055882353 | 10.48757305882353
Ic(4.3 K) | 275.5216 | 355.3407 | 448.6819 | 555.4507 | 678.3742 | 819.374 | 981.2073
Ic(1.96 K) | 442.6566 | 548.12 | 669.9007 | 755.2919 | 897.206 | 1058.512 | 1241.7848
Data 4.3 K | 555.4507 | 678.3742 | 819.374 | 981.2073
Data 1.96 K | 755.2919 | 897.206 | 1058.512 | 1241.7848
p =0.44* , q =1.85*
Fitting Ic data
BC2(4.3 K) = 23.73 T, C(4.3 K) = 43300 A T
BC2(1.96 K) = 25.93 T, C(1.96 K) = 51730 A T
Tc= 15.34 K
* B. Bordini, D. Richter, P. Alknes, A. Ballarino, L. Bottura, L. Oberli, - “Magnetization Measurements of High-Jc Nb3Sn Strands” - IEEE Trans. Appl. Superconduc., Vol. 23, No. 3, pp. 7100806, June 2013

## Slide 18: Critical Current (x strand) QXF Magnet
Chart: Peak Field, (T)
| 16.14 | 15.18 | 14.22 | 13.27562376470588 | 12.33730529411765 | 11.4078055882353 | 10.48757305882353
Ic(4.3 K) | 275.5216 | 355.3407 | 448.6819 | 555.4507 | 678.3742 | 819.374 | 981.2073
Ic(1.96 K) | 442.6566 | 548.12 | 669.9007 | 755.2919 | 897.206 | 1058.512 | 1241.7848
Ic(1.96K)*0.95 | 420.5237 | 520.714 | 636.4057 | 717.5273 | 852.3457 | 1005.5864 | 1179.6956
Magnet Load-Line | 0 | 436.5 | 488 | 531 | 585.7856
When fitted with the ITER Scaling Law, Transport Current Data seem confirming the reduced Tc observed in Magnetization Measurements
Table Courtesy of P. Ferracin
We gain 0.3 T (and 10 A), from 14.5 T to 14.8 T
Margin from
17.8 % to 19.3 %

## Slide 19: Conclusions
The procurement of the Nb3Sn wire is proceeding as planned
  Orders of conductor for prototype dipole magnets completed
  For the SMP of the QXF magnet all the orders have been placed and part of the wire already received at CERN (40 km RRP and 10 km PIT)
CERN has a significant experience with the 132/169 RRP wire: 88 Km of wire (from 18 billets) were procured for the FRESCA2 magnet and 40 km (from 10 billets) for the QXF magnets
First transport current measurements show that to scale (with the ITER scaling law) the temperature dependence of the critical current between 4.2 K and 1.9 K, we have to reduce the Tc at about 15.3 K
Margin from 17.8 % to 19.3 %

## Slide 20: Conclusions
The procurement of the Nb3Sn wire is proceeding as planned
  Orders of conductor for prototype dipole magnets completed
  For the SMP of the QXF magnet all the orders have been placed and part of the wire already received at CERN (40 km RRP and 10 km PIT)
CERN has a significant experience with the 132/169 RRP wire: 88 Km of wire (from 18 billets) were procured for the FRESCA2 magnet and 40 km (from 10 billets) for the QXF magnets
First transport current measurements show that to scale (with the ITER scaling law) the temperature dependence of the critical current between 4.2 K and 1.9 K, we have to reduce the Tc at about 15.3 K
Margin from 17.8 % to 19.3 %