## Slide 1: Bus Extender updates
Takashi Hachiya
Nara Women’s University & RIKEN BNL

## Slide 2: Status
Issues
  Making the through holes with Cu-plating
    Cu-Plating has nodules (wiggling surface)
    This could be caused by the residue of the glue when plating
      Glue is de-formed by the chemicals used for Cu-plating
  Low production yield – 20% from the prototype productions
Ideas to (try to) fix
  Change the glue sheet when laminating the layers
    Need to check the peel strength as well
  Update the production fixtures
    Vacuum pump, Cover sheets and sealing materials for vacuum-tight when exposure the substrate with the light to print the circuit.
    Company said that these work nicely and the production yields look improved
      No quantitative value is available yet.

## Slide 3: Peel strength measurement
Alisawa
Test 2 glue sheets which are specialized for LCP
  Panasonic, Arisawa
  Try 2 different pressures for the laminations
    Higher pressure is better?
Method
  Small sample (2 x 20cm)
  Use tensile tester with 180 degree
Results
  Panasonic ~ 3N/2cm,
  Alisawa ~ 40>/2cm
  Current (bad) glue 6N/cm
Alisawa is better than others
Panasonic
Current

## Slide 4: Through hole with Alisawa glue
We made the sample FPC with Alisawa glue and checked the through hole
  Alisawa shows good through holes
Hole before Cu-plating
Hole with Cu-plating

## Slide 5: Thermal shock test w/ Alisawa
Thermal shock test
  3 samples (one 400x, two 1000x)
    Connect multiple holes and measure its resistance
    If hole has damage by heat, the resistance get higher
  1000 cycle with -15 - 75C
    Temperature range is limited
    LCP is expanded by heat 2x more than polyimide
  Started from Apr. 9th
Bad case w/ current (bad) glue

## Slide 6: Status and Plan
Both issues are fixed (Test results shows)
New prototype production is in progress
  Plan to come by end of May
We measure their electrical performance
  Signal loss and reflection, cross talk, impedance
Next tests after the Corona shutdown
  radiation-hardness (facility is closed)
  Checking bubble if the problem still remains

## Slide 7: Eye-diagram of the bus extender
The eye diagram and bit-error rate with the prototype bus extender was measured
  No INTT module used, instead commercial LVDS driver (MAX9169)
BER ~ 10-9 is far from the mask