## Slide 1: UED-301650: UF82 Direct detection of dynamic pathways during photoinduced phase transition in VO2
PI: Junjie Li1, Yimei Zhu1
Collaborator: Jing Tao1, Lijun Wu1, Weiguo Yin, Olivier Delaire3
1. Condensed Matter and Material Science Division, BNL
2. Duke University
22nd ATF Users Meeting: Application for Continuation
Sponsored by the U. S. DOE, BES,
(Received)

## Slide 2: Unique optical/electric properties across phase transition in VO2
VO2 as thermosensitive switch in light-driven thermoelectric conversion system
Thermal conductivity across the metal-insulator transition
Ktot Total thermal conductivity
Ke electronic thermal conductivity.
Lee, S., Science 355, 371 (2017)
Zhang, Y., J. Mater. Chem. A 7, 8521 (2019)

## Slide 3: BNL MeV-Ultrafast Electron Diffraction
Acceleration voltage = 2.8 MeV
106 electrons per pulse
Temporal resolution ~ 180 fs
Notes: Here shows a typical optical pump probe measurement. The pump pulse will arrive first to initiate a dynamical process, This involves the interaction between laser and sample. Also it set the time-zero or the beginning of the whole process. Then after a short time-delay, at t1, the probe pulse arrives to measure the reflectivity. By adjusting the time delay, we finally can get a whole curve of how the optical properties change during the dynamic process initiated by the pump pulse.
Nowadays, there are many kinds of pump probe technique. They all use laser pulse to pump, but probe varies a lot.

## Slide 4: Sample preparation/TEM characterization
FIB
Monoclinic (300 K)
Rutile (350 K)
bulk VO2
Vanadium (Monoclinic)
Vanadium (Rutile)
Oxygen

## Slide 5: UED study of photoinduced phase transition
002
200
300
40-2
20-2
-102
-302
-504
0
2000 a. u.
(d)
-150 a.u.
200 a.u.
cM1
aM1
bM1
MeV-UED pattern before time zero, at 314 K
Differentiate the electron diffraction
at 730 ps
Monoclinic and Rutile phase
h0l with h=2n,
only Monoclinic phase
h0l with h=2n+1,
z
x

## Slide 6: Evolution of Individual Bragg Peak intensity
20 Monoclinic peaks
20 Rutile peaks
20 independent equations

## Slide 7: Atomic pathway of photoinduced phase transition in VO2
cM1
aM1
bM1
z
x
4 ps
Normal. displ. |z/z0|
0.05
0.05
0.1
|x/x0|
4 ps
4 ps
4 ps
0.025
Vanadium motion pathway
16 mJ/cm2
10 mJ/cm2
8 mJ/cm2

## Slide 8: UED measurement, 77K
No phase transition is found
until pump fluence of 16 mJ/cm2
Thermal heating matters

## Slide 9: No evidence for M2 in phase transition
Shao et al. NPG Asia Materials (2018) 10: 581-605
Electron diffraction pattern by UED

## Slide 10: Density-functional theory (DFT) Harmonic phonon dispersion calculations

## Slide 11: Summary
Confirm the photoinduced Monoclinic/insulator to Rutile/metal transition in single crystal VO2.
Discover the atomic path of structure phase transition in VO2
  A diagonal linear motion toward Rutile phase, ~ a few picosecond
  A V-V twisting dominant motion, deviating from diagonal direction, in ~100 ps
Find no evidence for existence of intermediate M2 in the phase transition
Thermal heating play an important role in the phase transition

## Slide 12
Thank You!

## Slide 13: Thermal transport at nanometer
Thermoelectric materials: MFP is too short
Nanometer scale materials: theory and regular measurement don’t work
Zeng, L., Scientific Reports 5, 17131 (2015)

## Slide 14: thermal transport in thermoelectric material Bi2Te3
Au
Bi2Te3
e-
1120
3030
e-p coupling and
phonon coupling within A
Phonon scattering and
Thermal transport at interface
Stuck by difficulty in the sample preparation